SECTION 10 71 13

ARCHITECTURAL SUN SHADES

United Enertech’s Sunshades offer energy savings by significantly lowering solar heat gain and reducing glare in the interior spaces. They also assist in the achieving LEED accreditation. United Enertech’s Sunshades also greatly affect the aesthetics of the building.

The specifier will need to edit this product specification for a specific project to reflect the desired options and applications.  The guide section has been written so that most editing can be accomplished by deleting unnecessary requirements.  Options are indicated by [   ].  Notes to assist the specifier in selecting options and editing the specification guide are printed in bold and indicated in Red { }.  For final editing, all brackets and notes will need to be deleted from the guide.

******************************************************************************

PART 1 - GENERAL

1.01	SUMMARY

A.	Section includes:  Modular, shop fabricated, metal sun shades to mount on exterior [window framing] [building walls] [_____].

B.	Related sections:

{List other specification sections dealing with work directly related to this section such as the following.}

1.	[Section 03 40 00 - Precast Concrete] [Section 04 20 00 - Unit Masonry] [Section 07 42 13 - Metal Wall Panels]:  Exterior wall surfaces to receive sun shades.

2.	[Section 08 41 00 - Entrances and Storefronts]  [Section 08 44 00 - Curtain Wall and Glazed Assemblies]:  Metal window framing to receive sun shades.

1.02	REFERENCES

{List by number and full title reference standards referred to in remainder of specification section.  Delete non-applicable references. }

A.	American Society for Testing and Materials (ASTM) Publications:

1.	ASTM A36 – Carbon Structural Steel.

2.	ASTM A500 - Cold-Formed Welded and Seamless Carbon Steel Structural Tubing in Rounds and Shapes.

3.	ASTM A526 - Sheet Steel, G-90 Zinc-Coated (Galvanized) by the Hot-Dip Process.

4.	ASTM A792 - Steel Sheet, Aluminum-Zinc Alloy-Coated (Galvalume) by the Hot Dip Process.

5.	ASTM B209 - Aluminum and Aluminum-Alloy Sheet and Plate.

6.	ASTM B221 - Aluminum Alloy Extruded Bar, Rod, Wire, Shape, and Tube.

7.	ASTM B117 - Standard Practice for Operating Salt Spray (Fog) Apparatus.

8.	ASTM D822 - Tests on Paint and Related Coatings Using Filtered Open-Flame Carbon-Arc Exposure Apparatus.

9.	ASTM D3363 - Test Method for Film Hardness by Pencil Test.

1.03	SUBMITTALS

A.	Provide in accordance with Section 01 33 00 - Submittal Procedures:

1.	Product data for sun shade components and finish.

2.	Shop drawings showing layout, dimensions, spacing of components, and anchorage and installation details.

3.	Calculations for support system.

4.	Sample:  [10” x 10”] [254mm x 254 mm] minimum size sample of sun shade panel illustrating design, fabrication workmanship, and selected color coating.

5.	Copy of warranty specified in Paragraph 1.05 for review by Architect.

1.04	QUALITY ASSURANCE

A.   Structural Requirements: Design, fabricate and install to support gravity loads and loads of related components as required for proper support and rigidity of configurations indicated, including provisions for deflection, expansion, and contraction forces.

B.   Certify that each welder employed in fabrication of work of this section has satisfactorily passed all AWS qualification test for welding processes involved.

C.   Installer qualifications:  Approved by manufacturer for installation sun of shade system and has a minimum of 5 years experience.

D.   Assemblers should conform to all applicable code requirements.

E.   Single Source Responsibility: Obtain sunshade device from one source of a single manufacturer.

1.05	WARRANTY

A.	Provide in accordance with Section 01 77 00 - Closeout Procedures:

1.	[ XX ] years warranty for factory finish against cracking, peeling, and blistering under normal use.

“XX” See United Enertech’s Finish Warranty & Maintenance Page for warranty time corresponding to type of finish selected.

PART 2 - PRODUCTS

2.01	ACCEPTABLE MANUFACTURERS

A.	United Enertech Corporation, 3005 S. Hickory St., Chattanooga, TN  37407;

423-698-7715.

B.	Requests to use equivalent products of other manufacturers shall be submitted in accordance with Section 01 63 00 - Product Substitution Procedures.

2.02	MATERIALS

{Edit this article to indicate if sun shade is fabricated from galvanized steel or aluminum.}

A.	Steel bar stock:  ASTM A36.

B.	Steel tubing:  ASTM A500, Grade B.

C.	Steel sheet:  ASTM A526 galvanized or ASTM A792 Galvalume.

D.	Extruded aluminum:  ASTM B221, Alloy 6063, Temper T6.

E.	Sheet aluminum:  ASTM B209 3003 or 5005, Temper T5.

F.    Fasteners shall be aluminum or stainless steel. Provide types, gauges, and lengths to suit unit installation conditions.

2.03	SUN SHADE SYSTEM

A.	Base of design shall be per Camana Series as manufactured by United Enertech Corporation.

B.   All components such as framing and mid-support tubes shall be 6063-T5 (T6) aluminum alloy.

C.	Framing shall be 2.25” x 2.25” X 0.081” square extruded aluminum tubing. Corners shall be fully welded to prevent any water penetration. Projections from the wall towards the outside of the building (sun shade) shall be [specify length (max. 48”) or as detailed on drawing]. Projections from the wall to the inside of the building (light shelf) shall be [specify length (max. 36”) or as detailed on drawing]. Special loads may require outriggers to be thicker materials on the outside of the building.

D.   Light shelf skin shall be a minimum of 0.0253” (22 gauge) to 0.25” (2 gauge) aluminum.  The light shelf skin shall be [solid, .31” dia. holes on 0.5” centers, consult United Enertech for additional hole patterns and centers available, specify hole diameter, pattern, and centers].

E.   Sun shade skin shall be a minimum of .0253” (22 gauge) to 0.25” (2 gauge) aluminum.  The sun shade skin shall be [solid, .31” dia. holes on 0.5” centers, consult United Enertech for additional hole patterns and centers available, specify hole diameter, pattern, and centers].

F.	Support system:  Provide framing/outriggers and mounting brackets or other means for support of sun shade panel fabricated from same material as panel.  System shall be designed to resist applicable dead, live, wind, and seismic loads. Size as required to provide sufficient structural support of panels.

G.	Fasteners:  Stainless steel bolts, studs, and other types of size and spacing as recommended by manufacturer for specific condition and detailed on approved shop drawings.

2.04	FACTORY FINISH

A.	Sun shade panels, outriggers, and other components shall receive applied coating heat cured to chemically bond finish to metal substrate as described in #3 below.

1.	Minimum hardness measured in accordance with ASTM D3363:  2H.

2.	Direct impact resistance tested in accordance with ASTM D2794:  Withstand 160 inch-pounds.

3.	Finish shall be {Choose one below}

- Mill Aluminum as provided from extruder.

- Powder Polyester TGIC, ([2 or 3*] coats), baked on at 410ºF, and meets AAMA-2603 Standards.

- Powder Super Durable Polyester, ([2 or 3*] coats), baked on at 410ºF, and meets AAMA-2604 Standards.

- Acrylic Baked Enamel (Acra-Bond Ultra) baked on at 350ºF and meets AAMA-2603 Standards.

- Kynar (Alum*A*Star), ([2 or 3*] coats), baked on at 450ºF, and meets AAMA 2605 Standards.

- Kynar 500 or Hylar 5000, 70% Trinar ([2 or 3*] coats), baked on at 450ºF, and meets AAMA 2605 Standards.

- Kynar 500 or Hylar 5000, 70% Tri-Escent II ([2 or 3*] coats), baked on at 450ºF, a blend of mica, ceramic, and inorganic pigments, and meets AAMA 2605 Standards.

- Clear Anodize 204 R-1 Class I (AA-C22A31)

- Clear Anodize 215 R-1 Class I (AA-C22A41)

- Integral Color Anodize  (AA-C22A42)

*3 coats denote a clear coat is applied to the color finish.

{United Enertech Corp. provides 24 standard colors.  Custom colors are available for minimum size orders.  Contact United Enertech Corp. for information on custom colors.}

B.	Color:  [[Bone White] [Polar White] [Sandstone] [Sierra Tan] [Antique Bronze] [Regal Brown] [Dark Bronze] [Burgundy] [Colonial Red] [Terra Cotta] [Cardinal Red] [Hemlock Green] [Slate Gray] [Interstate Blue] [Light Blue] [Matte Black] [El Cajon Silver] [Champagne] [Light Bronze] [Medium Bronze] as manufactured by United Enertech Corp.] [Selected by Architect from manufacturer's standard range.] [Custom color as selected by Architect.]

PART 3 - EXECUTION

3.01	PREPARATION

A.	Prior to fabrication, field verify required dimensions to ensure work will be accurately designed, fabricated, and fitted t the structure.

B.    Examine opening to receive sun shade. Do not proceed until any unsatisfactory condition has been resolved.

C.	Coordinate sun shade installation with provision of [exterior wall system] [window framing system] [curtain wall system] to ensure proper structural support is provided, attachment of sun shades is compatible with substrate, and weather tightness of exterior envelop is maintained.

3.02	INSTALLATION

A.	Install sun shades in accordance with manufacturer's installation instructions and approved shop drawings.

B.	Insulate dissimilar metals to prevent electrolysis with bituminous paint or non-absorptive gasket to prevent contact.

C.	Allow for thermal expansion and contraction of metal components.

D.	Install shade panels plumb, level, free from distortion, and aligned with building elements and adjacent shade panels.

E.	Do not install bent, bowed, or otherwise damaged panels.  Remove damaged components from site and replace.

F.	Attach shade panels to outriggers with appropriate fasteners for secure, permanent installation.

G.	After installation, touch-up damaged finish with paint supplied by manufacturer and matching original coating.

END OF SECTION